| CHEMICAL ENGINEERING TRANSACTIONS VOL. xxx, 2026 | A publication of |
| --- | --- |
|  | The Italian Association of Chemical Engineering Online at www.cetjournal.it |
| ### Guest Editors: Leonardo Tognotti, Rubens Maciel Filho, Viatcheslav Kafarov Copyright © 2026, AIDIC Servizi S.r.l. ISBN 979-12-81206-xx-x; ISSN 2283-9216 |  |

Green Synthesis of Ag Nanomaterials Using Microalgal Extracts for Photocatalytic Degradation of Contaminants: Experiments and Modeling

Federico Zedda a, Federico Atzori a, Silvia Casu a, Bartolomeo Cosenza b, Giacomo Fais a,c, Roberta Licheri a,c, Nicola Lai a,c, Francesco Desogus a,c, Rosangela Mastrangelo a, Giacomo Cao a,c, Alessandro Concas a,c,*

a Department of Mechanical, Chemical and Materials Engineering, University of Cagliari, Piazza d’Armi, 09123 Cagliari (CA), Italy

b Department of Civil and Industrial Engineering, University of Pisa, Largo Lucio Lazzarino, 56122, Pisa, PI, Italy

c Interdepartmental Centre of Environmental Science and Engineering (CINSA), University of Cagliari, Via San Giorgio 12, 09124 Cagliari, Italy

corresponding.alessandro.concas@unica.it

Synthetic dyes from industrial effluents are persistent pollutants requiring sustainable removal strategies. This study investigates the visible-light photocatalytic degradation of Brilliant Blue R using biogenic silver nanoparticles synthesized from microalgal extracts (Spirulina platensis and Chlorella vulgaris), reporting both experimental results and a hybrid modeling approach. Experimental analyses confirmed the effectiveness of the synthesized nanoparticles and their favorable physicochemical properties for photocatalytic applications. A simplified mechanistic model describing adsorption–desorption and degradation kinetics was developed to estimate key parameters, which were subsequently used to train artificial neural networks linking operating conditions to degradation performance. To address limited datasets, a Gaussian-noise-based augmentation strategy was introduced, significantly improving predictive accuracy. The proposed framework integrates experimental evidence with mechanistic and data-driven modeling, providing a reliable tool for optimizing sustainable photocatalytic processes based on microalgae-derived nanomaterials.

Introduction

Synthetic dyes widely used in textile, paper, and pharmaceutical industries are frequently discharged into wastewater, where their persistence and toxicity pose significant environmental and health risks (Zedda et al., 2026). These concerns highlight the need for sustainable and efficient treatment technologies (Peyghami et al., 2023). Photocatalytic degradation is a promising advanced oxidation process, exploiting semiconductor materials to generate reactive species capable of mineralizing organic pollutants. Metallic nanoparticles (NPs), due to their high surface area and distinctive physicochemical properties, enhance adsorption and catalytic performance. While metal oxides such as TiO₂ and ZnO are widely used, their activation is mainly limited to UV light (Pal and Kryschi, 2016). In contrast, silver nanoparticles (AgNPs) offer improved activity under visible light, making them more suitable for solar-driven applications (Syahirah Kamarudin et al., 2018).

Conventional chemical synthesis of AgNPs, albeit effective, often involves toxic reagents, prompting increasing interest in greener alternatives (Vidyasagar et al., 2023). In this context, microalgae-based synthesis represents a sustainable approach, as algal metabolites can act as both reducing and stabilizing agents (Sidorowicz et al., 2024a). Previous studies have demonstrated the effectiveness of AgNPs synthesized from microalgal extracts in degrading dyes such as Brilliant Blue R (BBR), although identifying optimal operating conditions remains challenging due to experimental limitations (Sidorowicz et al., 2024a; 2024b; 2025). To address this issue, this work combines experimental investigation with advanced modeling. A simplified deterministic model is developed to describe photocatalytic degradation by accounting for adsorption–desorption equilibrium and reaction kinetics, while retaining analytical tractability. Building on this, a machine learning model based on gradient boosting is developed to relate key operating variables, such as light intensity, dye concentration, nanoparticle dosage, and pH, to kinetic parameters, ensuring accurate and physically consistent predictions.

To overcome the scarcity of experimental data, a physics-consistent data augmentation strategy is introduced, incorporating uncertainty in both inputs and model-derived parameters (Cosenza et al., 2024). This hybrid framework enhances predictive capability while preserving mechanistic interpretability, providing a robust tool for optimizing photocatalytic processes based on sustainable, microalgae-derived nanomaterials.

Materials and methods

AgNPs were produced via a green synthesis route using microalgal extracts as natural reducing and stabilizing agents, following a previously reported procedure (Sidorowicz et al., 2024a; 2024b). In brief, the extracts of S. Platensis and C. vulgaris were reacted with an AgNO₃ solution under continuous stirring at elevated temperature, after which the nanoparticles were recovered, purified, and dried (Sidorowicz et al., 2025).

The photocatalytic degradation of BBR was investigated by varying key operating conditions, namely light intensity, catalyst loading, initial dye concentration, and pH. The catalyst was dispersed in a fixed liquid volume, sonicated, and mixed with BBR solutions, followed by a dark equilibration step prior to visible-light irradiation (Sidorowicz et al., 2024). During the experiments, the solution was continuously circulated through a flow-through cuvette connected to a UV-Vis spectrophotometer, enabling real-time monitoring of dye concentration over time. Spectral measurements were collected at regular intervals within the visible range.

A set of about 20 distinct experimental conditions (i.e. 10 for each strain) was explored by combining the selected operating variables, providing the dataset used for subsequent modeling summarized in Table 1.

Mathematical model

A mechanistically grounded model of moderate complexity is proposed to simulate experimental data, aiming to balance simplicity with physical realism. Following the approach of (Rasoulifard et al., 2016), the photodegradation process is described as a two-step mechanism: an initial adsorption of the pollutant onto the catalyst surface, followed by photocatalytic degradation of the adsorbed species once surface sites approach saturation. These steps can be schematically represented as follows:

| Dye⇌K1Dyeads | R1 |
| --- | --- |
| Dyeads→k3IS | R2 |

where Dyeads is the contaminant adsorbed on catalyst and Is the degradation products. Adsorption is modelled as a reversible reaction (R1) while the degradation reaction (R2) is considered irreversible. Accordingly in batch operated photocatalytic reactor, the relevant mass balances describing Dye degradation are:

| dDyedt=-k1Dye+k2Dyeads | (1) |
| --- | --- |
| dDyeadsdt=k1Dye-k2Dyeads-k3Dyeads | (2) |

along with the corresponding initial conditions Dye|t=0=Dye0 and Dyeads|t=0=0.  The closed-form solution of Eqs. (1–2), obtained as reported elsewhere (Atzori et al., 2025), is reported in Eq. (3) in terms of removal efficiency of the pollutant, i.e. η=1-DyeDye0.

| ηt=1-DyeDye0=1-12Δ-k1+k2+k3+Δe-Σ+Δ2t+k1-k2-k3+Δe-Σ-Δ2t | (3) |
| --- | --- |

where:

| Σ=k1+k2+k3 | (4) |
| --- | --- |
| Δ=Σ2-4k1k3 | (5) |

The parameters (k1), (k2), and (k3) were estimated by fitting the model to experimental data collected under 10 distinct operating conditions, each defined by specific combinations of light intensity, AgNP concentration, initial dye concentration, and pH. This resulted in a dataset of 10 parameter triplets per microalgal strain, yielding a total of 20 (k1, k2, k3) sets across the two strains investigated.

To search for a relation between the parameter values and the operating conditions values a machine learning approach is adopted by relying on the gradient boosting method. In particular, the predictive modeling workflow is developed to overcome the limited size of the experimental dataset by combining data augmentation with machine learning regression. Starting from the original measurements, an expanded dataset (≥400 samples) is generated through stochastic perturbation of both input and output variables. Specifically, input features ([NP], light intensity, pH, and initial dye concentration) are perturbed using a truncated Gaussian distribution bounded within ±5% of their nominal values, ensuring physically consistent variability. Output variables (k₁, k₂, k₃) are instead sampled from Gaussian distributions centered on the experimental means, with standard deviations equal to the reported measurement uncertainties, thus preserving the statistical structure of the experimental error. The augmented dataset is then split into training (80%) and validation (20%) subsets. A multi-output regression model is implemented by coupling GradientBoostingRegressor with MultiOutputRegressor, enabling simultaneous prediction of the 3 kinetic constants. Model training was performed using ensemble boosting of regression trees, with hyperparameters set to ensure a balance between bias and variance (e.g., number of estimators and learning rate). Model performance is evaluated on the validation set using standard metrics, including the coefficient of determination (R²), root mean squared error (RMSE), and mean absolute error (MAE).

Results and discussion

AgNPs are synthesized using microalgal extracts (e.g., S. platensis, C. vulgaris), where biomolecules act as reducing and stabilizing agents. The process involves nucleation, growth, and stabilization: metal ions are reduced to atoms, forming crystalline NPs. Biomolecules bind to crystal surfaces, guiding growth, and create a capping layer that prevents aggregation through steric and electrostatic effects, ensuring stable dispersion in solution (Sidorowicz et al., 2024c). A concise summary of the AgNPs characterization is provided by Atzori et al., (2025). XRD analysis confirm the formation of crystalline nanoparticles, with diffraction peaks corresponding to Ag, Ag₂O, Ag₂CO₃, and AgCl phases. Peak sharpness indicates good crystallinity, while broadening suggests nanoscale size (≈16.1 nm for C. vulgaris, ≈13.0 nm for S. platensis), with no impurities (Figure 1A).

Figure 1. Characterization of Ag NPs: XRD analyses (A). FTIR analysis (B).  TGA of Ag NPs from S. platensis (C) and C. vulgaris (D) extracts. Tauc plots of Ag NPs from S. platensis (E) and C. vulgaris (F).

TGA and FTIR analyses highlight the presence and role of organic biomolecules (Figure 1B). TGA reveales initial weight loss due to moisture removal, followed by decomposition of organic stabilizers, confirming their involvement in nanoparticle capping. Final residues (≈80% for S. platensis and ≈65% for C. vulgaris) correspond to the inorganic fraction (Figures 1C and 1D). FTIR spectra identify –OH and –C=O, which contribute to metal ion reduction and nanoparticle stabilization, with variations reflecting differences in extract composition (Gebre, 2023). UV–Vis analysis shows characteristic surface plasmon resonance peaks, confirming nanoparticle formation. Bandgap values (2.33 eV for S. platensis and 2.17 eV for C. vulgaris), indicate good visible-light absorption, with slight differences attributed to size, defects, and biomolecular interactions (Figures 1E and 1F).

Figure 2 shows the time evolution of dye removal during photocatalytic degradation using AgNPs from different microalgal strains under varying conditions (light intensity, initial concentration, catalyst loading, and pH).

Figure 2. Experimental and simulated (fitted) removal efficiencies under the investigated operating conditions using Ag NPs from S. platensis (SP), and C. vulgaris (CV) extracts.

High removal efficiencies are achieved under visible light, highlighting an advantage over UV-based systems. Experimental data and the analytical model (Eq. 3) are used to build the dataset for machine learning regression. Kinetic parameters (k₁, k₂, k₃) are estimated via Matlab (fminsearchbnd), with model fits closely matching experimental profiles. Optimized parameters’ values are reported in Table 1.

Table 1. Tuned values of deterministic model parameters obtained by fitting the experimental results.

| ID* | [NP] [mg L-1] | I [μEs-1m-2] | pH [/] | [Dye]0 [mg L-1] | k1 [min-1] | k2 [min-1] | k3 [min-1] |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SP_1 | 250 | 150 | 7 | 4 | 0.03694 ± 0.00068 | 0.05928 ± 0.0023 | 0.02974 ± 0.0017 |
| SP_2 | 250 | 150 | 7 | 18 | 0.005932 ± 0.00073 | 0.00744 ± 0.0025 | 0.2463 ± 0.0020 |
| SP_3 | 250 | 150 | 7 | 26.3 | 0.007374 ± 0.00075 | 0.059 ± 0.0025 | 0.03695 ± 0.0018 |
| SP_4 | 250 | 0 | 7 | 20 | 0.01236 ± 0.00073 | 0.06 ± 0.000 | 0.01472 ± 0.000 |
| SP_5 | 250 | 75 | 7 | 18.7 | 0.012 ± 0.00075 | 0.0526 ± 0.000 | 0.02147 ± 0.000 |
| SP_6 | 250 | 300 | 7 | 18.3 | 0.0119 ± 0.00063 | 0.06 ± 0.0018 | 0.0711 ± 0.0011 |
| SP_7 | 500 | 150 | 7 | 16 | 0.01746 ± 0.00055 | 0.006012 ± 0.0023 | 4.38∙10-5 ± 0.0015 |
| SP_8 | 125 | 150 | 7 | 18 | 0.0094 ± 0.00052 | 0.0370 ± 0.0021 | 0.01763 ± 0.0019 |
| SP_9 | 250 | 150 | 11 | 17.3 | 0.02433 ± 0.00069 | 0.0112 ± 0.0025 | 0.01938 ± 0.0011 |
| SP_10 | 250 | 150 | 3 | 18.3 | 0.009754 ± 0.0006 | 0.06 ± 0.002 | 0.05744 ± 0.0010 |
| CV_1 | 250 | 150 | 7 | 4 | 0.0193 ± 0.0015 | 0.0022 ± 0.0015 | (2.30 ± 0.22) ∙10-5 |
| CV_2 | 250 | 150 | 7 | 19 | 0.0201 ± 0.0016 | 0.004123 ± 0.0015 | (3.47± 0.34)∙10-11 |
| CV_3 | 250 | 150 | 7 | 33.3 | 0.0058 ± 0.0015 | 0.0166 ± 0.0014 | 0.0097 ± 0.0012 |
| CV_4 | 250 | 0 | 7 | 21 | 0.0023 ± 0.0011 | 0.01752 ± 0.0013 | 0.00167 ± 0.0009 |
| CV_5 | 250 | 75 | 7 | 20 | 0.0047 ± 0.0009 | 0.05952 ± 0.002 | 0.06911 ± 0.0012 |
| CV_6 | 250 | 300 | 7 | 17.3 | 0.0088 ± 0.0016 | 0.0034 ± 0.0009 | 0.6893 ± 0.0012 |
| CV_7 | 500 | 150 | 7 | 16.7 | 0.0298 ± 0.002 | 0.0015 ± 0.001 | (1.34 ± 0.08)∙10-7 |
| CV_8 | 125 | 150 | 7 | 20 | 0.0057 ± 0.0012 | 0.06 ± 0.0009 | 0.018 ± 0.0013 |
| CV_9 | 250 | 150 | 11 | 18 | 0.01121 ± 0.0014 | 0.0033 ± 0.0011 | 0.6832 ± 0.0009 |
| CV_10 | 250 | 150 | 3 | 18.7 | 0.00789 ± 0.0018 | 0.0588 ± 0.0015 | 0.01146 ± 0.0012 |

As previously described, starting from Table 1, an expanded dataset (≥400 samples) is generated for each strain by applying truncated Gaussian noise (±5%) to the input variables and Gaussian noise, based on experimental uncertainties, to the outputs. The dataset is then divided into training (80%) and validation (20%) subsets. A multi-output Gradient Boosting model is subsequently trained to predict k₁, k₂, and k₃. The resulting performance is reported in Figure 3 as parity plots and in Table 2 in terms of the main regression metrics.

Figure 3. Gradient Boosting simulation results (validation) in terms of parity plots of kinetic parameters k1, k2 and k3 for S. platensis (SP) and C. vulgaris (CV) using augmented data.

Overall, the model demonstrates high predictive capability for both systems, although with distinct trends depending on the target parameter and the microalgal strain.

Table 2. Performance metrics (R2, RMSE, and MAE) for Gradient Boosting regression applied to augmented data, categorized by strain (SP and CV) and parameters (k1, k2, k3).

| Strain | Param. | R2 | RMSE | MAE | Strain | Param. | R2 | RMSE | MAE |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SP | k1 | 0.989379 | 0.000965 | 0.000692 | CV | k1 | 0.880467 | 0.002980 | 0.002016 |
| SP | k2 | 0.910089 | 0.005854 | 0.003368 | CV | k2 | 0.917085 | 0.007218 | 0.003310 |
| SP | k3 | 0.816724 | 0.023750 | 0.011742 | CV | k3 | 0.999798 | 0.003034 | 0.001709 |

In the case of SP-derived nanoparticles, the model exhibits excellent performance for k₁ (R² ≈ 0.99), with very low error metrics, highlighting a strong predictive robustness for this parameter. The prediction of k₂ is comparable to the CV case (R² ≈ 0.91), indicating consistent model behavior across both systems. However, a noticeable decrease in performance was observed for k₃ (R² ≈ 0.82), accompanied by higher RMSE

For the CV-based system, the model achieves very high accuracy, particularly for k₃ (R² ≈ 0.9998), indicating an almost perfect agreement between predicted and experimental values. The predictions for k₁ and k₂ are also satisfactory (R² ≈ 0.88 and 0.92, respectively) in terms of low RMSE and MAE values, suggesting that the model effectively captures the underlying relationships despite experimental variability.

and MAE values, suggesting increased complexity or variability in the corresponding kinetics.

These results indicate that the proposed modeling framework is highly effective in capturing nonlinear relationships between process variables and kinetic parameters, while also highlighting system-dependent differences in predictability, likely associated with the physicochemical properties of the biogenic nanoparticles.

Conclusions

This study demonstrates that microalgae-mediated green synthesis is an effective route for producing Ag-based nanomaterials with strong photocatalytic activity under visible light. The synthesized nanoparticles, derived from Spirulina platensis and Chlorella vulgaris, shows favourable physicochemical properties and enabled high dye removal efficiencies across a range of operating conditions.

A simplified yet physically grounded kinetic model successfully describes the adsorption–desorption and degradation mechanisms, providing reliable parameter estimation. Coupling this mechanistic framework with a machine learning approach, supported by data augmentation, significantly enhances predictive capability despite limited experimental data. The Gradient Boosting model accurately captures nonlinear relationships between operating variables and kinetic parameters, achieving high performance metrics, particularly for selected parameters and strains.

Overall, the proposed hybrid methodology integrates experimental insights, mechanistic understanding, and data-driven modeling into a robust tool for process optimization. This approach not only improves the design of sustainable photocatalytic systems but also highlights the potential of microalgae-derived nanomaterials for environmentally friendly water treatment applications.

Nomenclature

[Dye] – contaminant concentration, mg/L

[Dye]0 – contaminant concentration, mg/L

k1, k2, k3 – kinetic constants, min-1

t – time, min

I – light intensity, mE/(m2·s)

η – removal efficiency, -

Acknowledgments

F.A., F.Z. and S.C. were supported by an International PhD Program in Innovation Sciences and Technologies at the University of Cagliari, Italy.

References

Atzori F., Cosenza B., Zedda F., Sidorowicz A., Fais G., Cao G., Concas A., 2025, Hybrid modeling of photocatalytic contaminant degradation using nanomaterials synthesized with microalgal extracts, Chemical Engineering Science, 316, 121945.

Cosenza B., Miccio M., Pannocchia G., Sammarco I., 2024, Advanced Simulation Model for Studying Biofuel-Producing Microalgae Populations. Chemical Engineering Transactions, 109, 559–564.

Gebre S.H., 2023. Bio-inspired Synthesis of Metal and Metal Oxide Nanoparticles: The Key Role of Phytochemicals. Journal of Cluster Science 34, 665–704.

Pal N.K., Kryschi C., 2016, Improved photocatalytic activity of gold decorated differently doped TiO2 nanoparticles: A comparative study, Chemosphere, 144, 1655-1664.

Peyghami A., Moharrami A., Rashtbari Y., Afshin S., Vosuoghi M., Dargahi A., 2023, Evaluation of the efficiency of magnetized clinoptilolite zeolite with Fe3O4 nanoparticles on the removal of basic violet 16 (BV16) dye from aqueous solutions, Journal of Dispersion Science and Technology, 44, 278-287.

Rasoulifard M.H., Seyed Dorraji M.S., Amani-Ghadim A.R., Keshavarz-Babaeinezhad N., 2016, Visible-light photocatalytic activity of chitosan/polyaniline/CdS nanocomposite: Kinetic studies and artificial neural network modelling, Applied Catalysis A: General, 514, 60-70

Sidorowicz A., Atzori F., Zedda F., Fais G., Loy F., Licheri R., Lai N., Desogus F., Cao G., Concas A., 2025. Novel experimental and theoretical study on the synthesis and use of microalgae-derived silver nanomaterials for water purification. Journal of Water Process Engineering, 69, 106831.

Sidorowicz A., Fais G., Desogus F., Loy F., Licheri R., Lai N., Cao G., Concas A., 2024a, Eco-Friendly Photocatalytic Treatment of Dyes with Ag Nanoparticles Obtained through Sustainable Process Involving Spirulina platensis, Sustainability, 16, 8758

Sidorowicz, Agnieszka, Fais, G., Desogus, F., Loy, F., Licheri, R., Lai, N., Locci, A.M., Cincotti, A., Orrù, R., Cao, G., Concas, A., 2024b, Optimization of Brilliant Blue R photocatalytic degradation by silver nanoparticles synthesized using Chlorella vulgaris, Environmental Science and Pollution Research, 31, 57765–57777.

Sidorowicz, Agnieszka, Yigit, N., Wicht, T., Stöger-Pollach, M., Concas, A., Orrù, R., Cao, G., Rupprechter, G., 2024c, Microalgae-derived Co3O4 nanomaterials for catalytic CO oxidation. RSC Advances, 14, 4575–4586.

Syahirah Kamarudin N., Jusoh R., Dina Setiabudi H., Fateha Sukor N., 2018, Photodegradation of methylene blue using phyto-mediated synthesis of silver nanoparticles: Effect of calcination treatment, in: Materials Today: Proceedings. https://doi.org/10.1016/j.matpr.2018.07.059

Vidyasagar N., Patel R.R., Singh S.K., Singh M., 2023, Green synthesis of silver nanoparticles: methods, biological applications, delivery and toxicity. Material Advances, 4, 1831–1849.

Zedda F., Atzori F., Casu F., Sidorowicz A., Fais G., Desogus F., Licheri R., Porcu S., Lutzu G.A., Cao G., Concas A., 2026, Green-Synthesized Ag/Zn Nanocomposites from Chlorella vulgaris Polar Extract: Sustainable Photocatalytic Water Remediation and Kinetic Modeling, Sustainability, 18(9), 4607.