| CHEMICAL ENGINEERING TRANSACTIONS VOL. xxx, 2026 | A publication of |
| --- | --- |
|  | The Italian Association of Chemical Engineering Online at www.cetjournal.it |
| ### Guest Editors: Leonardo Tognotti, Rubens Maciel Filho, Viatcheslav Kafarov Copyright © 2026, AIDIC Servizi S.r.l. ISBN 979-12-81206-xx-x; ISSN 2283-9216 |  |

Rice Husk Biochar for Tar Cracking: Critical Role of Minerals and Textural Properties

Adamu Mohammed Nafiua,*, Sangaré Diakaridiab, Van-de-steene Laurentb, Saleh Khashayara, Daouk Eliasa

a Université de technologie de Compiègne, École supérieure de chimie organique et minérale, Alliance Sorbonne Université, TIMR, Compiègne, France

bCIRAD BioWooEB, 73 Rue Jean-François Breton, 34398 Montpellier Cedex 5, France

mohammed-nafiu.adamu@utc.fr

This study investigates rice husk biochar for catalytic cracking of toluene - a tar model compound - in a fixed-bed reactor. The rice husk biochar was physically activated to about 25% conversion in either an H₂O or CO₂ atmosphere. The activated biochars were then employed as catalysts for toluene decomposition at 850 °C in a laboratory-scale fixed-bed reactor.

Catalytic performance evaluation of the raw rice husk biochar indicates poor activity in toluene cracking due to its low surface area and porosity. With physical activation, BET surface area increases significantly from 17 m2/g to 440 m2/g under CO2 and 426 m2/g under H2O. These morphological changes lead to better catalytic activity, particularly for the steam-activated char. It achieved about 71% toluene conversion and a longer activity span of about 20 min than the CO2-activated char, before total deactivation. This improved performance is attributed to the presence of surface mesoporosity, which slows deactivation. Silicon oxide constituted approximately 94 % of the inorganic content, which rendered the active metal species less effective in the process.

Introduction

Biomass valorization into bioenergy, such as syngas, has shown great potential. However, tar formation and impurity of the syngas remain major obstacles. Thermal cracking of the tar and use of naturally minerals as a catalyst for syngas purification have often proven inefficient and economically unviable (Huchon et al., 2024).

Biochar produced through thermochemical processes such as pyrolysis/gasification of lignocellulosic biomass, possesses properties that make it a potential heterogeneous catalyst. These include ultra-/super-microporosity and mesoporosity, the presence of transition metals and Alkaline and Alkaline earths metals (AAEM), as well as oxygenated surface functionalities (Frainetti and Klinghoffer, 2023; Klinghoffer et al., 2015). While porosity enhances gas diffusion to active sites, metals act as active sites, promoters, or supports (Claude et al., 2016). Surface functionalities are rarely considered due to their instability at high thermal treatment temperatures (Wood et al., 2024).

Previous studies indicated that woody biomass develops greater surface area during biochar production than agricultural waste, whereas the latter often possesses a higher inherent inorganic mineral content (Tomczyk et al., 2020). To further understand the influence of the surface porosities and presence of minerals in tar cracking, this study tends to compare the effectiveness of rice husk char and beech wood char for toluene cracking.

Experimental

2.1 Production, Activation, and characterization of Rice husk biochar (RHC)

Rice husk biomass (RHB) sample was initially sourced from Bama region of western part of Burkina Faso. The RHB sample was utilized in its original condition, without any pretreatment before biochar production, using a pilot-scale pyrolysis reactor at 900 °C under nitrogen atmosphere at 5 Nl/min and heating rate of 5 °C/min, followed by a holding time of 1 h. This high-thermal treatment aimed to produce stable char with less or negligible release of moisture content. Table 1 shows the results of physicochemical properties of the samples.

The produced biochar was subjected to a physical activation in a fixed-bed reactor using either 20 vol% CO2 (in N₂) at 900 °C or 20 vol% H2O at 800 °C. The differences in operating temperature between the H2O and CO2 experiments were due to the slow kinetic rate of the CO2 activation process (Arayedh et al., 2025a). Experiments were performed to reach a target carbon conversion of 25 %; CO₂ or H₂O injection was then stopped, and the flow was switched to 100 % N₂ to quench the reaction and cool the activated char to ambient temperature prior to collection. The carbon conversion (X) was calculated using the formula in equation 1. The product compositions were measured with micro gas chromatography (µ-GC).

X %= nc(t) Mcmo-mash×100   			(1)

where nc(t) is the cumulative number of moles of carbon content gases at a certain time (CO, CO2, CH4, C2H2, C2H4, C2H6) (mol), Mc is the molecular mass of carbon (g/mol), mo and mash denote the initial mass of biochar and ash content (g), respectively.

The raw biomass, produced biochar, and activated biochars were characterized for surface porosity (N2 and CO2 sorption isotherms) and for morphology using a scanning electron microscope (SEM). To further investigate the mineral composition and surface dispersion, scanning electron microscopy-energy dispersive X-ray spectroscopy (SEM-EDX) and inductively coupled plasma emission spectroscopy (ICP-OES) were also conducted.

Table 1: Physicochemical properties of the biomass and biochar.

|  | Rice husk biomass | Rice husk biochar |  |
| --- | --- | --- | --- |
| Proximate Analysis wt.% (db) |  |  |  |
| Volatile matter | 66.91 ± 0.15 | 1.99 ± 0.04 |  |
| Fixed carbon | 16.23 ± 0.37 | 56.07 ± 0.52 |  |
| Ash | 16.86 ± 0.02 | 41.93 ± 0.56 |  |
| Ultimate Analysis wt.% (db) |  |  |  |
| Carbon | 41.47 ± 0.01 | 54.37 ± 0.13 |  |
| Hydrogen | 4.69 ± 0.06 | 1.33 ± 0.05 |  |
| Nitrogen | 0.33 ± 0.03 | 0.4 ± 0.07 |  |
| Oxygena | 36.65 ± 0.08 | 1.9 ± 0.01 |  |

a by difference

2.2 Experimental setup

The toluene cracking experimental setup is depicted in Figure 1. The whole setup comprises a fixed-bed reactor, two cooling systems, electric heating resistances, a micro gas chromatography (µ-GC), a nitrogen flow meter, and a manometer. The fixed-bed reactor coupled with an electric furnace and consisted of two quartz glass reactors with internal diameters of 16 mm and 26 mm. The smaller quartz glass has a sintering disk with a thickness of 1 mm positioned as a catalyst bed. Both reactors are fixed onto a two-flange disk that differentiates the inlet and outlet flow of the gases, where the smaller quartz glass is inserted into the larger one. A temperature-controlled double enveloped cooling system comprises a glass bubbler-tube, thermocouple, and cooling agent (fluid) used for cooling down and maintaining the toluene liquid to -15 °C. A cooling bath comprising two glass bubblers filled with 100 mL of isopropanol, cooled to −20 °C, was used to trap condensable products at the reactor outlet. The permanent (non-condensable) gases passed through a µ-GC (Varian CP - 4900) for gas analysis. The condensable liquid products were analyzed using an Agilent GC/MS system.

Rice husk biochar, used as a catalyst, was initially placed in the inner quartz reactor, with a catalyst bed height of 13 mm, before assembling the system. The reactor was then purged with pure N₂ at a flow rate of 13.8 NL/ min while being heated at 20 °C/min up to a target temperature of 850 °C. Once a stable temperature of -15 °C was reached in the toluene cooling system, and the upstream and downstream heating lines were at 250 °C, nitrogen flow was passed through the toluene flask and then diverted directly to µ-GC to measure the toluene and verify its stability. The toluene concentration mostly stabilizes within the range of 4500-4800 ppm, depending on the room temperature, and it takes not fewer than 1 hour to achieve absolute stability with less average of 15 ppmv standard deviation. Afterward, the stable nitrogen and toluene flow was channeled back to the reactor through the catalyst bed with a contact time of 0.13 s. Condensable gases were collected in the cooling trap, as non-condensable gases were directed to and measured online with the µGC analyzer. During the experiments, coke deposited on the surface of the catalyst, which was collected and measured after stopping the toluene injection and cooling the system to an ambient condition with nitrogen flow. The toluene conversion (XT) was calculated using the formula in equation 2.

XT %=wT,in-wT,outwT,in×100   			(2)

where, wT,in is the amount of toluene molecule injected into the reactor (ppm, mol, g), and wT,out is the amount of toluene molecules collected out of the reactor (ppm, mol, g).

Figure 1: Schematic representation of toluene cracking experiment setup (Arayedh et al., 2025b).

Results and discussion

Biochars derived from rice husk (RHC) and beech-wood (BWC) were produced and characterized. These materials were subsequently physically activated to a carbon conversion of 25% using either H₂O (X25%-H₂O-RHC and X25%-H₂O-BWC) or CO₂ (X25%-CO₂-RHC and X25%-CO₂-BWC). The resulting activated chars, together with the raw rice husk biochar (Raw-RHC) and quartz glass beads (thermal cracking), were then used for toluene cracking, enabling a comparison between thermal and catalytic cracking effects, as discussed in sections 3.2.

3.1 Characterization of biochar and activated biochars

To examine the effect of physical activation on the textural properties of the produced biochar and activated biochars, N₂ sorption isotherms were evaluated, and the results are presented in Figure 1 and Table 2.

Figure 1: N2 adsorption-desorption isotherms of the raw biochar and activated samples.

The results indicate a significant increase in the specific surface area of the raw rice husk biochar, from 17 m2/g to 440 m2/g for CO2-activated char and 426 m2/g for H2O-activated char. Despite their similar specific surface area development, the steam-activated char developed greater mesoporosity due to its ability to widen existing pores, which resulting in a larger mesopore volume for both samples (Alvarez et al., 2014).Rice husk–activated biochars developed a lower specific surface area than activated beech-wood biochars, due to their higher ash content, especially the presence of Si in the RHC compared to BWC. This results in pore blockage and a dilution of surface area when expressed per gram of material (Tomczyk et al., 2020).

Table 2: N2 sorption isotherms analysis results.

| Biochar samples | Raw-RHC | X25%-CO2-RHC | X25%-H2O-RHC | X25%-CO2-BWC* | X25%-H2O-BWC* |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| BET Surface area (m2/g) | 17 | 440 | 426 | 582 | 600 |  |  |
| Micropore surface area (m2/g) | 15 | 317 | 316 | 540 | 452 |  |  |
| Mesopore surface area (m2/g) | - | 30 | 84 | - | - |  |  |
| Total pore volume (cm3/g) | - | 0.2007 | 0.2316 | 0.3294 | 0.3891 |  |  |
| Micropore volume (cm3/g) | 0.0054 | 0.1422 | 0.1258 | 0.2423 | 0.2054 |  |  |
| Mesopore volume (cm3/g) | - | 0.0293 | 0.0792 | 0.0460 | 0.1358 |  |  |

Results marked with an asterisk (*) were reported from Arayedh et al., (2025a)

Table 3 showed the results of ICP-OES analysis for the RH biomass and biochars produced and how the transformation from raw biomass to physical activation affects the inorganic metals composition. For all the rice husk-derived biochar, silica was the major inorganic element present with about 94% of silicon oxide, and minor content of other compounds such as AAEMs and transition metals. The activated biochars have nearly the same composition of inorganic metals retained, except for K, Ca, Fe, and Si.

Table 3: The elemental compositions of the samples (wt.% dry basis).

| Samples | RH Biomass | RH Biochar | X25%-CO2-RHC | X25%-H2O-RHC |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Na | <LD | <LD | <LD | <LD |  |  |
| Mg | 0.04 ± 0.01 | 0.09 ± 0.01 | 0.11 ± 0.01 | 0.12 ± 0.01 |  |  |
| Al | 0.07 ± 0.01 | 0.12 ± 0.01 | 0.15 ± 0.01 | 0.16 ± 0.01 |  |  |
| K | 0.26 ± 0.01 | 0.70 ± 0.02 | 0.87 ± 0.02 | 0.94 ± 0.01 |  |  |
| Ca | 0.13 ± 0.01 | 0.29 ± 0.01 | 0.34 ± 0.01 | 0.38 ± 0.02 |  |  |
| Ti | 0.01 ± 0.01 | 0.02 ± 0.01 | 0.02 ± 0.01 | 0.02 ± 0.01 |  |  |
| Mn | 0.01 ± 0.01 | 0.03 ± 0.01 | 0.04 ± 0.01 | 0.04 ± 0.01 |  |  |
| P | 0.04 ± 0.01 | 0.08 ± 0.01 | 0.10 ± 0.01 | 0.11 ± 0.01 |  |  |
| Si | 7.22 ± 0.50 | 18.29 ± 0.34 | 23.16 ± 0.10 | 24.47 ± 0.16 |  |  |
| Fe | 0.03 ± 0.01 | 0.04 ± 0.01 | 0.15 ± 0.01 | 0.10 ± 0.01 |  |  |

3.2 Catalytic cracking of toluene over a biochar-based catalyst

Prior to the catalytic cracking test, a blank experiment was conducted with 2 mm diameter of quartz beads glass to determine the extent of thermal efficiency of the bed at 850°C. The experimental results showed an average toluene conversion of 28.5 ± 2.7 %. A similar finding of 28 % toluene conversion was reported under the same operating conditions (Arayedh et al., 2025b). The corresponding thermal and catalytic cracking results are presented in Figure 2. The Raw-RHC showed a limited effect, with a toluene conversion of 29.8 ± 1.1 %, nearly the same value obtained for quartz beads, which represent the thermal cracking effect. The poor performance of Raw-RHC may be attributed to its limited catalytic properties. The physical activation using steam and CO2 has been reported to transform the catalytic activity of biochar by improving toluene cracking conversion (Frainetti and Klinghoffer, 2023). The 25% steam and CO2-activated RHC catalysts showed improved performance in toluene cracking, with similar conversion after 3 min test, 71.5 ± 2.6 % and 68.9 ± 3.0 % respectively. This was followed by a drastic deactivation slope, which was greater for the CO2-activated char compared with the steam-activated char. The rice husk-derived catalysts were then compared with beech-wood derived catalyst produced under the same operating conditions and employed for cracking under similar conditions. However, the beech-wood-derived catalyst exhibited better performance with 95.4 ± 0.5 % for CO2-activated and 96.0 ± 0.03 % for steam-activated samples, along with a prolonged catalytic activity.

Figure 2: Thermal and catalytic cracking of toluene molecules at 850°C using rice husk and beech-wood biochar-based catalyst. Each experiment point corresponds to the mean of replicate measurements, and the error bar represents the standard deviation.

3.3 Influence of the textural properties

Textural properties, such as surface area and pore structure, strongly influence toluene cracking by controlling reactant accessibility and diffusion within the catalyst. In line with this, initial catalytic tests with Raw-RHC showed limited activity, suggesting that increase in surface area and porosity were needed to improve its catalytic properties. Previous studies have reported that physical activation (both from H2O & CO2) significantly improved the surface area and porosity of beech-wood biochar-based catalyst (Arayedh et al., 2025a). The specific surface area and pore volume play a vital role in toluene cracking, by controlling the accessibility of toluene molecules with a kinetic diameter of 0.58 nm to active sites and toluene adsorption capacity (Frainetti and Klinghoffer, 2023). It is evident that the raw rice husk biochar, with 17 m2/g and micropore volume of 0.0054 cm3/g, showed a poor catalytic activity and rapid deactivation due to limited diffusion and adsorption capacity. Subsequently, the physical activation improved surface area and pore volume, which enhanced the catalytic performance, resulting in high toluene conversion, higher than 70 %, in the first 3 min for both the H2O and CO2-activated biochars, mainly due to their similarly developed specific surface area. However, differences in mesopore properties distinguished their deactivation behavior. The CO₂-activated biochar experienced faster deactivation, likely due to limited diffusion caused by coke deposition on less-developed mesopore surfaces, which created a barrier to interaction with active sites within the micropores. The development of mesoporosity plays a vital role in facilitating diffusion and contributes to the longer conversion of toluene under a biochar-based catalyst.

3.4 Influence of the inorganic mineral contents

The presence of certain inorganic minerals, such as silica and phosphorus, has been found to inhibit to certain catalytic activities, according to Frainetti and Klinghoffer (2023). However, the presence of AAEMs and transition metals has also been reported to promote the catalytic activity. This effect can be accessed by using a proposed inorganic composition metric ratio (Ca + K)/(Si + P). For all the rice husk derived biochar, silica was the most abundant major inorganic element, which may explain their lower performance in toluene cracking compared with the beech-wood catalyst with low or negligible silica content (Arayedh et al, 2025b). According to the ICP-OES elemental analysis in Table 3, the steam-activated char retained higher contents of AAEMs (K and Ca), whereas the CO2-activated biochar retained more Fe. However, when considering the inorganic catalytic activity metric, both steam and CO2-activated char have a similar value of approximately 0.06 which is well below 1. This reveals that the global inorganic mineral content of rice husk–derived biochars contributes to an inhibitory effect on toluene cracking.

Conclusion

In this paper, the rice husk-derived catalysts, comprising of raw biochar, H2O, and CO2-activated biochars, were tested for toluene cracking using a fixed-bed reactor. Among the three-rice husk-derived catalysts studied, the steam-activated char performed better due its longer-term activity. However, compared with the beech-wood-derived catalyst, the rice husk showed lower performance, due to their differences in textural properties and inherent inorganic content.

The surface area and porosity of RHC improved after physical activation with steam and CO2. Steam activation developed greater mesoporosity, which enhanced the diffusion network as well as adsorption capacity, leading to higher catalytic performance than the CO2-activated char. The high silica content appears to have adversely affected the catalytic contribution of inorganic minerals in rice husk derived biochars, resulting in lower toluene cracking performance compared with the activated beech-wood derived catalyst. Steam activation improved the textural properties of rice husk derived char, which may have contributed in its enhanced performance in toluene catalytic cracking.

Nomenclature

| X % | Carbon conversion rate | [%] |
| --- | --- | --- |
| nc(t) | Cumulative number of moles of carbon content gases at a certain time (t) | [mol] |
| Mc | Molecular mass of carbon | [g/mol] |
| mo | Initial mass of biochar | [g] |
| mash | Mass of ash content | [g] |
| XT % | Toluene conversion | [%] |
| wT,in | Amount of toluene at the reactor inlet | [ppm, mol, g] |
| wT,out | Amount of toluene at the reactor outlet | [ppm, mol, g] |

Acknowledgments

The research work was funded by région Hauts-de-France and CIRAD Montpellier, France. The authors would like to appreciate the technical support of Jeremy Valette from CIRAD Montpellier, Michael Lefebvre from TIMR-UTC, and Adama Konate from the Service of Physico-Chemical Analysis of UTC, Compiègne, for the contribution to success of the work.

References

Alvarez, J., Lopez, G., Amutio, M., Bilbao, J., & Olazar, M. (2014). Upgrading the rice husk char obtained by flash pyrolysis for the production of amorphous silica and high quality activated carbon. Bioresource Technology, 170, 132–137. doi.org/10.1016/j.biortech.2014.07.073

Arayedh, W., De Steene, L. V., Saleh, K., & Daouk, E. (2025). Role of activation progress on textural properties of biochar and their impact on tar cracking. Chemical Engineering Science, 315, 121877. doi.org/10.1016/j.ces.2025.121877

Arayedh, W., Van De Steene, L., Saleh, K., & Daouk, E. (2025). Catalyst deactivation of biomass-derived biochars during tar cracking: Role of porosity. Biomass and Bioenergy, 193, 107604. doi.org/10.1016/j.biombioe.2025.107604

Claude, V., Courson, C., Köhler, M., & Lambert, S. D. (2016). Overview and Essentials of Biomass Gasification Technologies and Their Catalytic Cleaning Methods. Energy & Fuels, 30(11), 8791–8814. doi.org/10.1021/acs.energyfuels.6b01642

Frainetti, A. J., & Klinghoffer, N. B. (2023). Recent experimental advances on the utilization of biochar as a tar reforming catalyst: A review. International Journal of Hydrogen Energy, 48(22), 8022–8044. doi.org/10.1016/j.ijhydene.2022.11.127

Huchon, V., Martin, E., Pinta, F., Commandré, J. M., & Van De Steene, L. (2024). Conversion in a char bed reactor of tars and syngas from a wood gasifier. Energy, 288, 129738. doi.org/10.1016/j.energy.2023.129738

Klinghoffer, N. B., Castaldi, M. J., & Nzihou, A. (2015). Influence of char composition and inorganics on catalytic activity of char from biomass gasification. Fuel, 157, 37–47. doi.org/10.1016/j.fuel.2015.04.036

Tomczyk, A., Sokołowska, Z., & Boguta, P. (2020). Biochar physicochemical properties: Pyrolysis temperature and feedstock kind effects. Reviews in Environmental Science and Bio/Technology, 19(1), 191–215. doi.org/10.1007/s11157-020-09523-3